Internal QC: 1x Screw Cell

Order Description

| Client |  |  |
| --- | --- | --- |
| Order # |  |  |
| Order component description | Screw Cell 1x |  |
| Version | 1.3RC HN 5mm rev4 |  |
| Number of items / Start date |  |  |
| Batch # |  |  |

Final QC Checklist :

| # | Procedure | Check |
| --- | --- | --- |
| 1 | No significant geometry defects: - High fidelity of CAD model features - Surface parallelism, especially at component contact points - No significant gashes or chips - Cell alignment pins are intact and cell components align |  |
| 2 | No significant chip interface region damage: - Mostly smooth chip well, tolerance for occasional small area defects - Mostly smooth chip compression ring, tolerance for occasional singular defects of low depth (i.e. <50um, grit 240 sandpaper grain size) |  |
| 3 | No significant production residues: - No resin residues: sticky, smooth shiny spots that have a different texture from surroundings especially in chip interface regions, channels, and electrolyte wells - No sanding residues: grainy, powdery patches that may be rolling free or well-adhered to the material, especially in chip interface regions, channels, and electrolyte wells |  |
| 4 | Channels free of obstruction and flush with IPA or DI |  |
| 5 | Fastener features free from obstruction, M2 screws and nuts clamp cell securely |  |
| 6 | Quantitative geometry check: - Length of cell assembly >25.8mm and < 27.3mm - Width/height > 15.8mm and < 16.2mm - (Sample cell) Min chip well X,Y > 5.05mm and < 5.2mm |  |
| 7 | Final check: - Pass cell if meets #1 – 6 - Internal use only if meets #1 – 6, but doubts with #1, #6 and cosmetic issues; more than occasional #2 problems but may still be usable; fully cured resin residues in #3a, some permanent residues in #3b but not in fluidic interface regions - Fail if falls outside of above |  |

Notes (#pass/internal use only/fail, additional procedures, modifications, etc.):

| QC operator: | Finished date: |
| --- | --- |